## Slide 1: “聆听”半导体中的电子自旋噪声 “Listening” to the spin noise of electrons in semiconductors
杨鲁懿
清华大学物理系
luyi-yang@mail.tsinghua.edu.cn

## Slide 2
2003-2007 清华大学 学士
2007-2013 美国加州大学伯克利分校 博士
2013-2016 美国国家强磁场实验室Los Alamos 博士后
2016-2019 加拿大多伦多大学物理系 助理教授
2019.9-今 清华大学物理系 副教授
CV

## Slide 3
应用和发展
先进光学技术
凝聚态物理
Research Area
Please visit http://info.phys.tsinghua.edu.cn/yanglab/ for more information.

## Slide 4
事情是这样的…
8字班吴致颉同学
续老师的课超赞哦!
那今年大作业选这个话题吧！
Notes: 我的毕业设计从中受益匪浅

## Slide 5
About noise
Black: 单次测量
Red：100次平均
N次测量平均的噪声
However
Not all noise in experimental measurements is unwelcome.
Certain fundamental noise sources contain valuable information about the system itself.

## Slide 6
Fluctuation–dissipation theorem
When there is a process that dissipates energy, turning it into heat (e.g., friction), there is a reverse process related to thermal fluctuations.
Drag and Brownian motion
Resistance and Johnson noise
Notes: quantifies the relation between the fluctuations in a system that obeys detailed balance and the response of the system to applied perturbations.
If an object is moving through a fluid, it experiences drag (air resistance or fluid resistance). Drag dissipates kinetic energy, turning it into heat. The corresponding fluctuation is Brownian motion. An object in a fluid does not sit still, but rather moves around with a small and rapidly-changing velocity, as molecules in the fluid bump into it. Brownian motion converts heat energy into kinetic energy—the reverse of drag.
If electric current is running through a wire loop with a resistor in it, the current will rapidly go to zero because of the resistance. Resistance dissipates electrical energy, turning it into heat (Joule heating). The corresponding fluctuation is Johnson noise. A wire loop with a resistor in it does not actually have zero current, it has a small and rapidly-fluctuating current caused by the thermal fluctuations of the electrons and atoms in the resistor. Johnson noise converts heat energy into electrical energy—the reverse of resistance.

## Slide 7
“Noise spectroscopy”: a simple example
Simple mechanical system: Cantilever (diving board)
What’s resonant frequency (ω0)?
What’s ringdown time (Q)?
F

## Slide 8
“Noise spectroscopy”: a simple example
Simple mechanical system: Cantilever (diving board)
What’s resonant frequency (ω0)?
What’s ringdown time (Q)?

## Slide 9
“Noise spectroscopy”: a simple example
Simple mechanical system: Cantilever (diving board)
What’s resonant frequency (ω0)?
What’s ringdown time (Q)?

## Slide 10
How to measure electron spin dynamics?
Method 1: Perturbative methods (e.g. optical pump-probe)
Method 2: Nonperturbative methods (e.g. optical spin noise spectroscopy)
z
z

## Slide 11
Beam splitter
Delay stage
Dt
Transient reflectivity
pump
probe
Ultrafast pump-probe spectroscopy “Freeze” time on femtosecond timescales
Notes: With the development of femtosecond laser systems the ultrafast time scales (below one nanosecond) are accessible, even in small laboratory experiments.

## Slide 12
k
G
E
qK~ (n - n)
Measure electron polarization
Energy
Absorption
RCP
LCP
0
aRCP
aLCP
Index of refraction
0
nRCP
nLCP
0
0
Optical spin orientation and
Faraday/Kerr rotation spectroscopy
pump

## Slide 13
Pump
Time delay
Faraday rotation
S
Spin projection along k
Inject spin polarization optically and measure its lifetime
Notes: 光子有两种自旋态，方向是沿着光传播的方向，平行或反平行，左旋/右旋对应的角动量是正负1。

## Slide 14
Faraday rotation
Inject spin polarization optically and measure its lifetime
S
B
Voigt geometry
Q: What would happen in a transverse magnetic field?
Larmor precession
Notes: 扭转力

## Slide 15
Inject spin polarization optically and measure its lifetime
Normally, spin dynamics revealed with spin-resonance (NMR, ESR),pump-probe optics: techniques are necessarily perturbative

## Slide 16
Inject spin polarization optically and measure its lifetime
Normally, spin dynamics revealed with spin-resonance (NMR, ESR),pump-probe optics: techniques are necessarily perturbative
Bloch equation

## Slide 17
Dynamics also available via stochastic “spin noise”
Spectrum of correlations:
Dr. Scott Crooker

## Slide 18
Nonperturbative measurement
Probe laser can be tuned far from absorption, but still measure spin via n+-n-
In this regard, it is “non-perturbing” probe

## Slide 19
Experimental setup

## Slide 20
Experimental setup

## Slide 21
interval, Nm
Relaxation time
1/(sampling rate)
Measurements
require the calculation of ∼Nm2 products
average over i

## Slide 22
power spectrum
Noise power spectrum
Additivity: the contributions from independent noise sources add to each other.
Scales as ~Nm
Wiener–Khinchine theorem: in the steady state, the noise power spectrum and the spin–spin correlator are related by the Fourier transform:
autocorrelation

## Slide 23
interval
Relaxation time
1/(sampling rate)
F.T. spectrum
F.T. spectrum
F.T. spectrum
average over all results
Measurements

## Slide 24
Spin noise in n-GaAs
Spin noise signals are small! 10-1000x less than photon shot noise (nanoradians/√Hz)
PRB 79, 035208 (2009)
Additivity: the contributions from independent noise sources add to each other.

## Slide 25
Spin noise in n-GaAs
PRB 79, 035208 (2009)

## Slide 26
Spin noise in n-GaAs
PRB 79, 035208 (2009)

## Slide 28
References
GaAs: PRB 79, 035208 (2009)
Alkali atomic gas (K, Rb, Cs): Nature 431, 79 (2004)
InGaAs quantum dots: PRL 108, 186603 (2012)
Two-color spin noise: Nat. Commun 5, 4949 (2014); Sci. Rep. 5, 9573 (2015)
Higher-order spin noise: New. J. Phys. 15, 113038 (2014)
Review: Rep. Prog. Phys 79, 106501 (2016)

## Slide 29: Inhomogeneous and homogeneous linewidths of self-assembled QDs
The homogeneous linewidths are inaccessible by conventional linear optical spectroscopies.
New technique: 2-color SNS to probe below the inhomogeneous broadening.
LINEAR technique!
Notes: 10^10 /cm^2 x20L 10% hole

## Slide 30: Spin noise in InGaAs quantum dots with a single probe
The laser is very sensitive to fluctuations on Dot A, but not sensitive to fluctuations on Dot B.
PRL 104, 036601 (2010), PRL 108, 186603 (2012).
QD A
QD B

## Slide 31: 2-color spin noise spectroscopy
Different dots: Uncorrelated noise, add incoherently.
Same dots: Correlated noise, add coherently!
The FR variance (i.e., the measured FR noise power):

## Slide 32: 2-color spin noise setup
F.T.

## Slide 33: 2-color SNS measurements
Uncorrelated, noise signals add incoherently
Correlated, noise signals add coherently
Notes: 1pm = 1.5ueV = 375 MHz @900nm, 500kHz -> 300ns

## Slide 34: 2-color spin noise correlator
Correlated
Uncorrelated
The correlator has a Lorentzian line shape, and its HWHM is the homogeneous linewidth.
Correlated
Uncorrelated

## Slide 35: Laser intensity dependence
gamma_h increases with the intensity due to the resonant QD pumping effects and excitation-induced broadening.

## Slide 36: Temperature dependence
gamma_h broadens with increasing temperature in QDs due to interactions with phonons.

## Slide 37: Control experiment on bulk n-GaAs
Correlator is independent of detuning.
Notes: 3.7x10^16/cm^3

## Slide 38
power spectrum
Noise power spectrum
Additivity: the contributions from independent noise sources add to each other.
Scales as ~Nm
Wiener–Khinchine theorem: in the steady state, the noise power spectrum and the spin–spin correlator are related by the Fourier transform:
autocorrelation
Cross-correlation
spin densities with different indexes

## Slide 39
D1 transition
795nm
895nm
Faraday rotation
Two-color SNS to reveal spin interactions in multi-component spin systems

## Slide 40
F.T.
Experimental setup
Spin noise power spectra
Cross-correlation spectra

## Slide 41
Spin noise power spectra and
cross-correlation spectra
arXiv:1408.5399
F.T.
F.T.